## Slide 1
Durability of Metal Halide Perovskites in Simulated Space Environments
Zoe Bell, Arizona State University
Principal Investigator: Nicholas Rolston, Arizona State University
Graduate Mentor: Saivineeth Penukula, Arizona State University

## Slide 2
MHPs
  Perovskite solar cell
  Power conversion efficiency
  Thin and lightweight
Must withstand stressors such as high radiation exposure across the solar spectrum
Metal Halide Perovskites (MHPs)
Honsberg, C., & Bowden, S. (n.d.). Properties of light. In Properties of sunlight. PV Education. Retrieved July 28, 2025, from https://www.pveducation.org/pvcdrom/properties-of-sunlight/properties-of-light
Figure 1. Image of perovskite atomic structure
Notes: Metal halide perovskites (MHPs) are thin, lightweight ionic conductors emerging as a promising material for photovoltaics. Compared to traditional solar cells made of silicon or group III-V elements, MHPs are more affordable, flexible, and offer competitive power conversion efficiency. For space applications, however, they must withstand stressors such as high radiation exposure across the solar spectrum, including UVA, UVB, and UVC.

## Slide 3
IPA Submersion Nonsubmerged
0 hr
12 hr
24 hr
48 hr
72 hr
96 hr
100 hr
Perovskite Exposure to UVA, UVB, UVC
Acknowledgement: This material is based upon work primarily supported by the National Science Foundation under award No.ECCS-2025490.
UVA
UVB
UVC
Notes: In my study, I prepared four perovskites—CsPbI₃ with 5% PVP (submerged in IPA), CsPbI₃ with 5% PVP (non-submerged), MAPbI₃, and CsPbI₃∙FAI—and exposed each to UVA, UVB, and UVC radiation, documenting their characteristics over 100 hours.

## Slide 4
Creating a Uniform Film
Figure 4. Spin Coater with Gas Quenching
Figure 5. Annealed Substrates
Figure 3. UVO Cleaner
Figure 2. Ultrasonic Cleaner
Figure 6. Olympus Microscope
Figure 7. Photoluminescence (PL) Spectrometer
Figure 8. UVB Lamp
Notes: The two perovskites solutions I made were Cesium Lead Iodide doped with Formamidinium Iodide and methylammonium lead triodide. To prepare the substrate, ITO coated glass slides were initially cleaned with an industrial-grade soap solution of extran and water. After sonication, the ITO-coated glass was cleaned with deionized water and a brush to remove the residual soap. . Then, the ITO-coated glass was cleaned with IPA and acetone for 10 min in that order. Finally, the ITO-coated glass was cleaned with UV Ozone treatment for 15 min.
After that, the ink is prepared inside of a nitrogen glove box. Perovskite on top ITO-coated glass and glass was fabricated using spin coating and gas quenching. 200 µL of perovskite precursor solution was deposited on the cleaned substrate, which was then spin-coated and gas quenched at pressure of 50 psi. The films were annealed on a hot plate for 15 minutes. Finally, PVP was applied via spin coating. Adding small layer of PMMA to prevent moisture to simulate space condition

## Slide 5
Visual Impact of UVC Exposure
UVC |  | 
Sample | Before (0 Hours) | After (100 Hours)
IPA Submersion |  | 
Nonsubmerged |  | 
UVC |  | 
Sample | Before (0 Hours) | After (100 Hours)
Polymethyl methacrylate (PMMA) applied via spin coating
Direct exposure
  No protective structure such as glass
Color change signaled degradation
Acknowledgement: This material is based upon work primarily supported by the National Science Foundation under award No.ECCS-2025490.
Notes: The most damaging UV condition was UVC. Before testing, the perovskite films were coated with polymethyl methacrylate (PMMA) via spin coating. Their dark black color indicated that the films were in their most efficient, light-absorbing form. When CsPbI₃∙FAI turned yellow, it signaled degradation into lead iodide—a non-functional phase for solar cells.The samples had direct exposure to the light. None of the samples had protective layers like glass, which would absorb light and shield the perovskite.

## Slide 6
PL Changes in UVC
Acknowledgement: This material is based upon work primarily supported by the National Science Foundation under award No.ECCS-2025490.
UVC Range: 100 nm – 280 nm
Chart: UVC CsPbI3 5% PVP IPA Submersion
Chart: UVC CsPbI3 5% PVP Nonsubmerged
Chart: UVC Cs0.2FA0.8PbI3
Chart: UVC MAPI
Notes: While observing results from the photoluminescence (PL) spectrometer, I focused on a shift in wavelength either decreasing or increasing and observed the degradation of the peaks over time. UVA (315–400 nm), UVB (280–315 nm), and UVC (100–280 nm) represent increasing radiation energy levels, simulating conditions found in low Earth orbit.

## Slide 7
Wavelength Shifts of Perovskites
A wavelength shift signals instability and compositional change
Chart: UVC Wavelength Shift
| 0 | 12 | 24 | 48 | 72 | 96 | 100
CsPbI3 5% PVP IPA Submersion | 692.5 | 697.5 | 702 | 696.5 | 694 | 694 | 693.5
CsPbI3 5% PVP Nonsubmerged | 697.5 | 697.5 | 697.5 | 695 | 695 | 684 | 694
MAPbI3 | 772.5 | 767.5 | 769.5 | 762.5 | 774 | 772 | 771
Cs0.2FA0.8PbI3 | 785 | 793.5 | 799 | 806 | 807 | 804.5 | 802
Chart: UVB Wavelength Shift
| 0 | 12 | 24 | 48 | 72 | 96 | 100
CsPbI3 5% PVP IPA Submersion | 695 | 696.5 | 697.5 | 694 | 696.5 | 699 | 696.5
CsPbI3 5% PVP Nonsubmerged | 695.5 | 696.5 | 694 | 692 | 694 | 695 | 696.5
MAPbI3 | 772 | 772 | 770.5 | 773.5 | 781.5 | 772 | 771
Cs0.2FA0.8PbI3 | 791 | 788 | 793.5 | 791.5 | 798.5 | 798.5 | 806.5
Chart: UVA Wavelength Shift
| 0 | 12 | 24 | 48 | 72 | 96 | 100
CsPbI3 5% PVP IPA Submersion | 697 | 693.5 | 694 | 694 | 694.5 | 695 | 695
CsPbI3 5% PVP Nonsubmerged | 696 | 697 | 695 | 695 | 695.5 | 694 | 697
MAPbI3 | 772 | 772 | 770.5 | 773 | 774 | 771 | 776
Cs0.2FA0.8PbI3 | 785.5 | 785.5 | 783 | 819.5 | 819.5 | 817 | 810
Acknowledgement: This material is based upon work primarily supported by the National Science Foundation under award No.ECCS-2025490.
Notes: Our goal is to see no shift in wavelength and either consistent or increasing PL intensity. A shift in wavelength indicates that the perovskite is degrading. Since UVC caused the greatest amount of wavelength shifting, this supports the conclusion that UVC was the most damaging of the three radiation types. MAPbI₃ showed the least amount of wavelength shifting, while CsPbI₃∙FAI showed the most.
MAPbI₃ showed the least amount of wavelength shifting, while Cs_0.2 FA_0.8 PbI_3 showed the most across all UV exposures.

## Slide 8
Degradation Rate of Photoluminescence (PL) Intensity Over Time
Chart: Degradation Rate of PL Intensity in UVA
| 0 | 12 | 24 | 48 | 72 | 96 | 100
CsPbI3 5% PVP IPA Submersion | 100 | 20.6371 | 20.0662 | 12.9139 | 11.6556 | 9.7351 | 10.7285
CsPbI3 5% PVP Nonsubmerged | 100 | 16.8449 | 10.2139 | 7.0053 | 7.4866 | 6.5241 | 6.8449
MAPbI3 | 100 | 25.2372 | 32.4478 | 41.9355 | 53.8899 | 50.6641 | 47.0588
Cs0.2FA0.8PbI3 | 100 | 67.2922 | 69.3029 | 23.307 | 23.3244 | 35.9249 | 48.1233
Chart: Degradation Rate of PL Intensity in UVB
| 0 | 12 | 24 | 48 | 72 | 96 | 100
CsPbI3 5% PVP IPA Submersion | 100 | 17.5 | 8.75 | 8.5368 | 4.0441 | 4.3088 | 4.5368
CsPbI3 5% PVP Nonsubmerged | 100 | 8.9503 | 4.2652 | 3.5525 | 2.8343 | 2.1934 | 2.4144
MAPbI3 | 100 | 6.6254 | 5.8481 | 7.5442 | 4.5406 | 11.8551 | 18.9046
Cs0.2FA0.8PbI3 | 100 | 23.2716 | 66.0802 | 17.5309 | 4.9321 | 15.8642 | 16.358
Chart: Degradation Rate of PL Intensity in UVC
| 0 | 12 | 24 | 48 | 72 | 96 | 100
CsPbI3 5% PVP IPA Submersion | 100 | 2.3905 | 1.1524 | 1.2476 | 0.19048 | 0.25619 | 1.2381
CsPbI3 5% PVP Nonsubmerged | 100 | 4.9943 | 2.1761 | 1.7102 | 0.25398 | 0.625 | 0.88636
MAPbI3 | 100 | 14.0377 | 13.7866 | 9.3933 | 8.3473 | 14.3096 | 13.1381
Cs0.2FA0.8PbI3 | 100 | 27.5 | 34.7 | 317 | 611 | 481 | 634
Sharp increase due to temporary trap state formation
Notes: The significant increase in the degradation rate of CsPbI₃∙FAI may reflect the temporary effects of trap state formation during degradation. Shallow trap states can act as radiative recombination centers, leading to increased PL despite ongoing degradation. However, it is important to note the wavelength shift and the change in film color, as these indicate that degradation products will continue to form until the PL eventually drops.

## Slide 9
Final Observations
UVC |  |  | 
Sample | Avg. Wavelength Shift (nm) | Avg Degradation Rate (%) | Overall Stability
 | 3.07 | -87.83 | Most Stable
Nonsubmerged | 3.14 | -98.22 | Stable
IPA Submersion | 3.75 | -98.92 | Moderately Stable
 | 17.07 | 221.30 | Least Stable
UVC |  |  | 
Sample | Avg. Wavelength Shift (nm) | Avg Degradation Rate (%) | Overall Stability
 | 3.07 | -87.83 | Most Stable
 | 3.14 | -98.22 | Stable
 | 3.75 | -98.92 | Moderately Stable
 | 17.07 | 221.30 | Least Stable
UVC was the most damaging of the three radiation types
MAPbI₃ showed the least amount of wavelength shifting, while showed the most

## Slide 10
Next Steps
Material selection for space-based solar applications
Tailoring MHP compositions for specific radiation environments
Acknowledgement: This material is based upon work primarily supported by the National Science Foundation under award No.ECCS-2025490.
Kirmani and Sellers, Are metal-halide perovskite solar cells really radiation tolerant?, Joule (2025), https://doi.org/ 10.1016/j.joule.2025.101852
Notes: UVC caused the greatest wavelength shifts, the most noticeable color changes, and a rapid, sharp drop in photo response across all compositions. These results support the conclusion that UVC was the most damaging of the three radiation types.

## Slide 11
Acknowledgement: This material is based upon work primarily supported by the National Science Foundation under award No.ECCS-2025490.
Acknowledgements
I would like to thank Nicholas Rolston and Saivineeth Penukula for scientific guidance and helpful discussions.
This material is based upon work supported by the National Science Foundation under award No. ECCS-2025490. Experimental work was conducted at Arizona State University Research Park MacroTechnology Works facility.

## Slide 12
Kirmani, A. R., & Sellers, I. R. (2025). Are metal-halide perovskite solar cells really radiation tolerant? Joule, 9(3). https://doi.org/10.1016/j.joule.2025.101852
Masi, S., Canale, C., Ferretti, A. M., Manca, M., & Listorti, A. (2023). Atomic arrangement in (a) CsPbI₃ and (b) MAPbI₃ elementary cell [Figure]. ResearchGate. https://www.researchgate.net/figure/Atomic-arrangement-in-a-CsPbI3-and-b-MAPbI3-elementary-cell_fig1_371566593
Nguyen, H., Penukula, S., Mahaffey, M., & Rolston, N. (2024). All inorganic CsPbI₃ perovskite solar cells with reduced mobile ion concentration and film stress. MRS Communications. https://doi.org/10.1557/s43579-023-00510-7
Segovia, R., Qu, G., Peng, M., Sun, X., Shi, H., & Gao, B. (2018). Evolution of photoluminescence, Raman, and structure of CH₃NH₃PbI₃ perovskite microwires under humidity exposure. Nanoscale Research Letters, 13(1), 79. https://doi.org/10.1186/s11671-018-2470-0
Xiong, H., DeLuca, G., Rui, Y., Qia, J., Li, Y., Zhang, Q., Wang, H., & Reichmanis, E. (n.d.). Modifying perovskite films with polyvinylpyrrolidone for ambient-air-stable highly bendable solar cells. Unpublished manuscript.
References

## Slide 13
PL Changes in UVA
UVA Range: 315 nm – 400 nm
Chart: UVA CsPbI3 5% PVP IPA Submersion
Chart: UVA CsPbI3 5% PVP Nonsubmerged
Chart: UVA Cs0.2FA0.8PbI3
Chart: UVA MAPI
Notes: While observing results from the photoluminescence (PL) spectrometer, I focused on a shift in wavelength either decreasing or increasing and observed the degradation of the peaks over time. UVA (315–400 nm), UVB (280–315 nm), and UVC (100–280 nm) represent increasing radiation energy levels, simulating conditions found in low Earth orbit.

## Slide 14
PL Changes in UVB
UVB Range: 280 nm – 315 nm
Chart: UVB CsPbI3 5% PVP IPA Submersion
Chart: UVB CsPbI3 5% PVP Nonsubmerged
Chart: UVB Cs0.2FA0.8PbI3
Chart: UVB MAPI

## Slide 15
Total Irradiance
  the total amount of solar energy that falls on a unit area
Trapezoidal Rule – Calculating Irradiance
  Standard Spectra
  Area = (x₂ - x₁) * (y₁ + y₂) / 2
  Summed all trapezoid areas total irradiance (W/m²)
  =
Chart: ASTM E-490 AM0 Standard Spectra Adjusted UVC
| 244.5 | 245.5 | 246.5 | 247.5 | 248.5 | 249.5 | 250.5 | 251.5 | 252.5 | 253.5 | 254.5 | 255.5 | 256.5 | 257.5 | 258.5 | 259.5 | 260.5 | 261.5 | 262.5 | 263.5 | 264.5 | 265.5 | 266.5 | 267.5 | 268.5 | 269.5 | 270.5 | 271.5 | 272.5 | 273.5 | 274.5 | 275.5 | 276.5 | 277.5 | 278.5 | 279.5 | 280.5
 | 0.06097 | 0.04939 | 0.0504 | 0.0555 | 0.04565 | 0.05638 | 0.0601 | 0.04601 | 0.04155 | 0.05155 | 0.05957 | 0.0793 | 0.1018 | 0.1254 | 0.1251 | 0.104 | 0.08551 | 0.0898 | 0.1036 | 0.1658 | 0.2497 | 0.2527 | 0.2494 | 0.2508 | 0.2438 | 0.2389 | 0.2673 | 0.2244 | 0.1974 | 0.1965 | 0.1326 | 0.1751 | 0.2428 | 0.2338 | 0.1593 | 0.08555 | 0.09463
 | 0.06097 | 0.04939 | 0.0504 | 0.0555 | 0.04565 | 0.05638 | 0.0601 | 0.04601 | 0.04155 | 0.05155 | 0.05957 | 0.0793 | 0.1018 | 0.1254 | 0.1251 | 0.104 | 0.08551 | 0.0898 | 0.1036 | 0.1658 | 0.2497 | 0.2527 | 0.2494 | 0.2508 | 0.2438 | 0.2389 | 0.2673 | 0.2244 | 0.1974 | 0.1965 | 0.1326 | 0.1751 | 0.2428 | 0.2338 | 0.1593 | 0.08555 | 0.09463
Solar Energy Estimate for LEO
Notes: The unit W*m-2*nm-1 represents spectral irradiance, which is the power of electromagnetic radiation per unit area per unit wavelength. Specifically, it measures the radiant power (in Watts) incident on a surface per square meter (m²) and per unit wavelength (in nanometers (nm)). It essentially quantifies the amount of radiant power at a specific wavelength arriving at a surface.
Sticker on bottom, film side up.
UVB restesting for PL
Only the 2 hour submersion, PMMA iw
Check every 12 – 16 hours.
Take out
MAPI (2)
CsPbI_3
With PVP PMMA
Without PVP all with PMMA

## Slide 16
UV Exposure vs. LEO Environment
UV | Irradiance (W/m²) | Time (s) | Energy (J) | LEO Equivalent
UVA | 0.646 |  |  | 
UVB | 0.991 |  |  | 
UVC | 2.332 |  |  | 
UV | Irradiance (W/m²) | Time (s) |  | LEO Equivalent
UVA | 0.646 |  |  | 
UVB | 0.991 |  |  | 
UVC | 2.332 |  |  | 
=
Formula for calculating energy per unit area based on irradiance and time.
Acknowledgement: This material is based upon work primarily supported by the National Science Foundation under award No.ECCS-2025490. 16