## Slide 1
Noah Zheng, Washington University in St. Louis
Catherine Ott, Northwestern University
PI: Dr. Ian McCue, Northwestern University
Coarsening Kinetics of Nanoporous, Tantalum-Based UHTCs

## Slide 2: Overview: Ultra-High Temperature Ceramics
Nitrides, carbides, and borides of a refractory metal (e.g., Ta, Nb, Mo, W)
Favorable characteristics:
  High melting point
  High thermal conductivity
  High mechanical stiffness
Wyatt et al, Nat. Rev. Mater., 2024
> 3700
3017
3090

## Slide 3: Overview: Ultra-High Temperature Ceramics
Suitable for hypersonic applications
  Vehicles that travel > 5x speed of sound
  Extreme heat flux and oxidation conditions
Peters et al, Nat. Comm., 2024

## Slide 4: Nanoporous UHTCs Enable Novel Functionality
Active Cooling
  e.g. Transpiration cooling: forced fluid through porous structure
Peters et al, Nat. Comm., 2024

## Slide 5: How Do Nanoporous UHTCs Hold Up?
Nanoporous structures "coarsen" at high temps due to surface diffusion
Obtain kinetic constants D0, E, and m
Courtesy of Ian McCue and Catherine Ott

## Slide 6: Project Approach
Nanoporous Source Powder
Coarsening
X-Ray Diffraction (XRD)
Scanning Electron Microscopy (SEM)
Phase Stability
Feature Size Measurements
1400, 1550, 1700, 1850 °C
5, 10, 30, 60 minutes
Induction Heating:
Ta (Metal)
TaC (Ceramic)

## Slide 7: Induction Heating Allows For Precise Coarsening
TaC
Ta

## Slide 8: Compositional Stability of TaC

## Slide 9: Compositional Stability of Ta

## Slide 10: Coarsening: Visual Progression

## Slide 11: Coarsening: Visual Progression

## Slide 12: Feature Size Quantification with AQUAMI
TaC, 1550 °C, 5 minutes
4 μm.

## Slide 13: Feature Size Quantification with AQUAMI
4 μm.

## Slide 14: Challenges with Feature Size Measurement in Ta
Ta, 1550 C, 60 minutes
3 μm
3 μm

## Slide 15: Ta Source Powder Inconsistency
4 μm.

## Slide 16: Kinetic Analysis

## Slide 17: Kinetic Analysis
m = 3 suggests bulk crystal diffusion
m = 4 suggests surface diffusion
(Balluffi et al, 2005)

## Slide 18: Conclusions
TaC coarsens at a significantly slower rate than Ta
Preliminary m-values suggest bulk crystal diffusion and surface diffusion
log(diameter) vs. log(duration) seems linear for Ta coarsening

## Slide 19: Moving Forward
Improving Ta sample consistency:
Dealloyed Source Powder
Commercial Source Powder (Dehydriding)
2 μm
2 μm

## Slide 20: Moving Forward
Improving Ta sample consistency:
Dealloyed Source Powder
Commercial Source Powder (Dehydriding)
Molybdenum Susceptor
Graphite Susceptor
TaN
New materials:
Kinetic Analysis for TaC:
Lengthened Coarsening Durations

## Slide 21: Acknowledgments
This work made use of the Northwestern University Jerome B. Cohen X-ray Diffraction Core Facility (RRID:SCR_017866) supported by the MRSEC program of the National Science Foundation (DMR-2308691) at the Materials Research Center of Northwestern University and the Soft and Hybrid Nanotechnology Experimental (SHyNE) Resource (NSF ECCS-2025633).
This work made use of the EPIC facility (RRID: SCR_026361) of Northwestern University’s NUANCE Center, which has received support from the SHyNE Resource (NSF ECCS-2025633), the IIN, and Northwestern's MRSEC program (NSF DMR-2308691).