## Slide 1: Stretchable Vertical Organic Electrochemical Transistors
Joohwan Choe
Mentor: Ayush Dhande
PI: Dr. Antonio Facchetti
NSF Award: 2349519

## Slide 2: Introduction – What is an OECT?
Organic Electrochemical Transistor
Low Driving Voltage
Mixed Ionic-Electronic Conduction
High Transconductance
Polymer Flexibility
Notes: Make slide 2 and 3 same.
What oect is, how it works, its properties and reasons for its properties,

## Slide 3: OECT Device Mechanics
Device Mechanic
Gate Voltage drives ions from electrolyte into the organic semiconductor
Causes a change in the semiconductor doping state
Allows the electrons to flow from Source to Drain for transistor to function
https://www.ossila.com/pages/organic-electrochemical-transistors-oects

## Slide 4: Why are OECTs important?
Li B, Wang Y, Mei J et al. Wearable Bioelectronics: Toward Future Personal Health Monitoring. BIO Integration 2026; 7: 1–10.

## Slide 5: Why is it Stretchable and Vertical?
Stretchability for wearable electronics as human strain experiences strain of 30%
Vertical OECT overcomes the fabrication limit and reduces source & drain distance
Substrate
Bottom electrode
Semiconductor channel
Top electrode
Notes: Stretchability part, to incorporate it onto human skin must be able to stretch while functioning. Diff methods to make these devices stretchable. You can intrinsically or extrinsically modify them to be more stretchable by using more stretchable materials or changing the overall geometry of the OECT.
Planar limited by the fabrication limitations.

## Slide 6: Research Project: Optimization of N-type OECT
Reference gate
Electrolyte
PEDOT:PSS electrode
Supporting Layer
Active Channel
Micro-crack Electrode
Stretchable Substrate
Organic Semiconductor
SEBS
Bottom Au
HOMO-gDPPTz
Top Au
PEDOT:PSS
SEBS
Micro-cracked Au
S
S
S
S
O-H
O-H
O-H
O-H
O-S=O
O-S=O
Molecular Bridge
Au supporting layer
PEDOT:PSS
Notes: This is the cross-section of the OECT. Explain the structure of the device.
Gold is the major issue (least stretchable) explain it: delamination between layer …

## Slide 7: OECT Fabrication Process
Clean Glass Slide
Spin-Coat Dextran
Drop-Cast SEBS
Evaporate micro-cracked Au
Spin-Coat semiconductor
Evaporate Au supporting layer
SAM on Au
Spin-coat PEDOT:PSS
Au
HOMO-gDPPTz
Glass
Dextran
SEBS
Au
PEDOT:PSS
Whole Device
Glass
Glass
Dextran
Glass
Dextran
SEBS
Glass
Dextran
SEBS
Au
HOMO-gDPPTz
Glass
Dextran
SEBS
Au
Au
HOMO-gDPPTz
Glass
Dextran
SEBS
Au
Au
HOMO-gDPPTz
Glass
Dextran
SEBS
Au
Au
HOMO-gDPPTz
Glass
Dextran
SEBS
Au
PEDOT:PSS

## Slide 8: Roadmap of my data
03
Bottom Electrode
Resistance vs strain on microcracked Au
Top Electrode
Bonding between self-assembled monolayer and Au
Organic Semiconductor
N-type polymer photo crosslinked for improved stretchability
Ion Selectivity
K+ and pH testing to indicate the selectivity of our devices
8
Notes: My contributions: Resistance vs strain graph of bottom electrode, SAM test using XPS, rigid N and P-type performances, rigid N type OECT with PEGDMA, K and pH testing for the rigid PEGDMA devices.

## Slide 9: Bottom Electrode

## Slide 10: Bottom Electrode – Microcracked Au
100 µm
0%
50%
100%
3 cm
Optical images taken by Ayush Dhande
Embedded gold into the SEBS substrate (stretchable base)
Formation of microcracked Au enabling conductivity
10

## Slide 11: Top Electrode

## Slide 12: Top Electrode – XPS
Cysteamine and Au (S-Au) bond formation in the range of 161.9 – 162.2 eV
XPS confirmed that the bond was present
Cysteamine and Au bond
S
S
S
S
H2N
H2N
H2N
H2N
O-S=O
O-S=O
Molecular Bridge
Au supporting layer
PEDOT:PSS
12

## Slide 13: Organic Semiconductor

## Slide 14: Organic Semiconductor
Homo-gDPPTz crosslinked to PEGDMA at varying concentrations for improved ductility without electrical performance degradation
14

## Slide 15: I-V plot of an OECT
15
I-V plot of an OECT
Transconductance (gm)
performance metrics of OECT that measures the amplification ability

## Slide 16: Photo crosslinked N-type Semiconductor
95 N-type semiconductor to 5 PEGDMA does not cause performance degradation
60 x 60 µm devices
100/0 PEGDMA
95/5 PEGDMA
90/10 PEGDMA
16
Notes: Concluded that 95/5 ideal volume ratio for n-type OECT

## Slide 17: Ion Selectivity

## Slide 18: Potassium (K+) Ion Selectivity
95/5 PEGDMA
Ion selective membrane was adsorbed onto the 95/5 PEGDMA device
Test was conducted to measure the OECT’s performance to detect K+ ions selectively
Maintained consistent high transconductance value
Potassium Ion Selectivity
18

## Slide 19: Potassium (K+) Ion Selectivity
95/5 PEGDMA
19
100/0 PEGDMA

## Slide 20: pH Selectivity
100/0 PEGDMA
pH selectivity measured at pH ranging from 4.5 – 10
Decrease in pH led to more H+, allowing the transfer curve to peak higher
Confirmed its ability to selectively detect different pH values
pH Selectivity
20

## Slide 21: Conclusion and Future Work
Successfully processed N-type HOMO-gDPPTz OECT device with high transconductance, stretchability, and selectivity
The 95:5 (HOMO-gDPPTz:PEGDMA) ratio showed minimal degradation while 90:10 ratio still showed high transconductance value (~60 gm)
Future work, plan to fabricate a full electrical device capable of sensing K+, NH3, pH, glucose, electrical signal
21

## Slide 22: Acknowledgements
Dr. Antonio Facchetti
Ayush Dhande
Dr. Mengge Wu
Facchetti Lab
Dr. Mikkel Thomas
Leslie O’Neill
NSF (Award Number: 2349519)

## Slide 23: Questions?