## Slide 1: Nanoimprinted Laser Cavities on Silicon
April McLane
Home institution: Georgia Institute of Technology
Host institution: North Carolina State University
Mentor: Md Ayenul Azim, North Carolina State University
PI: Qing Gu, North Carolina State University

## Slide 2: Hybrid Organic-Inorganic Metal Halide Perovskites as Laser Gain Medium
Perovskites have properties such as long charge carrier lifetimes, high charge carrier mobilities, high quantum yields, tunable bandgaps, and high absorption coefficients1
Promising for use as gain media in lasers
Okumura, R. et. al. Chemistry Proceedings 2022, 9 (1), 11.
1Moon, J. et. al. ACS applied materials & interfaces 2021, 13 (4), 5368-5378.

## Slide 3: Motivation: Patterning Perovskites into Laser Cavities
The patterned perovskite film functions as the gain medium and the optical cavity
Optical cavities: confine light within the laser structure
  Patterned perovskite can be used as optical cavities to provide feedback and stimulated emission

## Slide 4: Nanoimprint Lithography (NIL) for Patterning Perovskite Films
Conventional patterning techniques (e.g. photolithography & e-beam lithography) use polar solvents that degrade perovskites2
NIL uses heat and pressure to pattern the perovskites
REU project goal: verify imprinting on glass and silicon with a flat stamp before moving to a patterned grating stamp
Long-term goal: create photonic crystal cavity structures on perovskite thin films
2Moon, J. et. al. ACS Photonics 2022, 9 (6), 1984-1991.

## Slide 5: NIL Method

## Slide 6: Stamp Preparation
Flat Si stamp coated with FDTS (an anti-adhesion layer)
  Needed for clean stamp release after imprinting
Contact angle measured to confirm hydrophobicity (>100o needed for clean release)

## Slide 7: NIL Procedure
MAPbBr3 thin films prepared on glass and Si substrates by Dr. Xiaotong Li’s group
Imprinted with flat stamp at 100oC, 70 bar for 20 minutes

## Slide 8: Results: Contact Angle
Average contact angle 104.49o (left: 102.42o, right: 106.57o)
Meets the >100o hydrophobicity criterion for clean stamp release

## Slide 9: Results: Imprinting on Glass Substrates
Before
After
Sample #1
Sample #2

## Slide 10: Results: Imprinting on Silicon Substrates
Before
After
Sample #1
Sample #2

## Slide 11: Conclusion & Future Work
Nanoimprinter reliably reaches target processing conditions (100oC, 70 bar) with MAPbBr3 on Si
FDTS-coated flat stamp met hydrophobicity requirement for clean release
Films on glass substrates showed no visible changes after imprinting
Films on silicon substrates had a visible outline after imprinting
  Some FDTS transfer from stamp to film
Future work: characterization (e.g., photoluminescence and SEM) of films before and after imprinting to evaluate imprint success

## Slide 12: Thank You!
Thank you to my mentors, Md Ayenul Azim and Prof. Qing Gu, for their guidance throughout this project as well as Dr. Xiang-Bin Han, Dr. Boyu Guo, and Prof. Xiaotong Li. Thank you to the RTNN REU program for the opportunity.
Contact email: amclane6@gatech.edu
This material is based upon work which is supported by the National Science Foundation (award numbers 2447827, 2447828, 2447829 and ECCS-2025064). Any opinions, findings, and conclusions or recommendations expressed in this material are those of the author(s) and do not necessarily reflect the views of the National Science Foundation.