## Slide 1
Degradation of Hydrogels for Lymphatic Drug Delivery
Heidi Thompson SUIN 2026
Mentor: Marianne Esnaurrizar
PI: Dr. Susan Thomas

## Slide 2
Introduction
  What is a hydrogel?
  Network of cross-linked polymers
  Retain large amounts of water
1
  What is the lymphatic system?
  Second circulatory system
  Acts as a drainage system
  Surveillance of the immune environment
(Ho, Tzu-Chuan et al., 2023, MDPI Molecules)

## Slide 3
Purpose of Hydrogel
2
(Lucas et al., 2025, ACS Nano)
(Kim et al., 2022, Nature Communications)
Created in https://BioRender.com
  Drug delivery system capable of enabling sustained drug release of small molecules into the lymphatic system
  Treat lymphatic diseases
Notes: size range appropriate for efficient lymphatic uptake (10–100 nm)
Simple loading of diverse drug types, administration without surgery
Lymphedema – lymphatic vessels stop pumping fluid
in situ - in the original place (place where treated)

## Slide 4
  Triblock copolymer
  Has hydrophilic and hydrophobic regions
  Forms micelles above specific concentration and temperature
Polymer A
(Li, Shanshan et al., 2023, International Journal of Nanomedicine)
3
Protein B
  Has acidic (carboxyl) and basic (amine) functional groups
  Very reactive, allows for chemical cross-linking
Notes: two FDA-approved polymers
amphiphilic - possesses both hydrophilic and hydrophobic regions/properties
amphoteric - acidic (carboxyl) and basic (amine) functional groups

## Slide 5
4
 | Polymer A | Protein B | Hydrogel
Biocompatible |  |  | 
Forms micelles |  |  | 
Stable |  |  | 
Gelation Temperature | High | Low | Above room temperature
Material Properties
Notes: Thermosensitive - liquid at low temperatures and gels above room temperature
Weight percent for cmc??

## Slide 6
  Degradation forms micelles that carry drugs to the lymphatic system
  Does varied temperature change the stability of the hydrogel?
  Where are components A and B in the degraded samples
Degradation of Hydrogel
5
(Wu, Jinghua et al., 2024, MDPI Gels)
Notes: (Sodium Dodecyl Sulfate-Polyacrylamide Gel Electrophoresis)

## Slide 7
Objectives
6
  Simulate degradation of hydrogel in physiological conditions
  Determine effects of different temperature storage conditions on degradation time and composition
  Characterize components of hydrogel degradation in supernatant using SDS-PAGE, iodine assay, and BCA assay
Notes: (Sodium Dodecyl Sulfate-Polyacrylamide Gel Electrophoresis)

## Slide 8
  A heat-cool cycle was performed: solubilized hydrogel was placed in the fridge and then warmed to room temperature three times
  Collected samples at hour 1, 2, 4, 7 (Day 0), and then once per day until fully degraded
Methods
7
Created in https://BioRender.com
Notes: Supernatant is the liquid above the hydrogel – PBS plus micelles that come off hydrogel

## Slide 9
Control data collected by Dr. Megan Elliott
8
  Hydrogel used immediately after solubilizing had 7-day degradation time
  Hydrogel that underwent heat/cool cycle had a 5-day degradation time
Effects of Thermocycling on Degradation Times
Chart: Degradation of 6% Hydrogel
| 0 | 1 | 2 | 4 | 7 | 24 | 48 | 72 | 96 | 120 | 144 | 168
Control | 1 | 1.1187 | 1.2251 | 1.2075 | 1.0325 | 1.0836 | 0.73692 | 0.5676 | 0.34998 | 0.3629 | 0.17648 | 0.080424
Heat/cool | 1.1508 | 1.3588 | 1.167 | 1.0758 | 1.2038 | 0.76662 | 0.66432 | 0.387 | 0.44138 | 0.16845 | 0 | 0

## Slide 10
  SDS-Polyacrylamide Gel Electrophoresis (SDS-PAGE)
    Iodine stains for polyethylene glycol (PEG) (Polymer A)
    Coomassie blue stains for proteins (Protein B)
Iodine assay to detect PEG (Polymer A)
Bicinchoninic acid (BCA) to detect proteins (Protein B)
Characterization of Degraded Samples
9
Notes: used to separate proteins based on their molecular weight
SDS page is for proteins
agarose is for DNA RNA

## Slide 11
SDS-PAGE
(PageRulerTM Unstained Protein Ladder 2 X 250 μL | Thermo ScientificTM.)
  Separates proteins based on size
  Smaller proteins migrate faster due to less resistance from the gel matrix
  4-20% Tris HCl protein gels were run at 180 V for 25 minutes
10
Created in https://BioRender.com
Notes: (Sodium Dodecyl Sulfate-Polyacrylamide Gel Electrophoresis)
- heat to denature
- detergent (SDS) to unfold proteins and give them a uniform negative charge
- electricity to push them through a gel mesh
- separation by size

## Slide 12
Iodine Stain: 24-Hour Timepoint
11
Polymer A
Polymer B
50/50 A:B
Sample 1
Sample 2
Sample 3
Polymer A is present in both controls and all three supernatant samples
Blank control lane (Protein B) is empty
Notes: Talk about controls!!
10 mg/ml polymer A
2.5 mg/ml polymer B

## Slide 13
200
150
120
100
85
70
60
50
kDa
12
Coomassie Blue Stain: 24-Hour Timepoint
Polymer A
Polymer B
50/50 A:B
Sample 1
Sample 2
Sample 3
Protein Ladder
  Protein B is 75 kDa
  Smearing indicates Protein B is present in samples
  Control reads ~60 kDa
  Supernatant lines ~65 kDa
Notes: Potentially smaller fragments?
Presence of gelatin causes smearing

## Slide 14
13
  PEG reacts with BaCl2 and Iodine to form color
  Measured absorbance at 535 nm
Chart: Concentration of Polymer A in Degradation Supernatant
| 0 | 1 | 2 | 4 | 7 | 24 | 48 | 72 | 96 | 120 | 144
Sample 1 | 2.7198 | 2.1815 | 2.5105 | 3.3081 | 5.5513 | 9.1007 | 5.6411 | 1.8026 | 0.60618 | 0.63609
Sample 2 | 1.663 | 3.3878 | 2.3011 | 5.6211 | 5.3519 | 6.1097 | 6.3988 | 2.8794 | 3.6072 | 2.8096
Sample 3 | 1.5833 | 1.6132 | 5.1426 | 6.1894 | 4.5743 | 5.1825 | 4.3151 | 3.1685 | 3.328 | 1.1545
Standard Curve
Iodine Assay
Notes: Pluronic started at 45mg/ml
days 1, 2, 3 had highest amounts of degradation

## Slide 15
  Colorimetric detection of total protein
  Measured absorbance at 562 nm
14
Chart: Concentration of Protein B in Degradation Supernatant
| 1 | 2 | 4 | 7 | 24 | 48 | 72 | 96 | 120 | 144
Sample 1 | 0.77774 | 0.92059 | 1.1729 | 0.7833 | 1.5625 | 0.87607 | 0.2898 | 0.061596 | 0.0096475
Sample 2 | 0.68868 | 1.043 | 0.60705 | 1.5403 | 0.8 | 1.6924 | 1.0857 | 0.8705 | 0.91874 | 0.60705
Sample 3 | 0.72393 | 0.66642 | 1.1395 | 1.5273 | 0.76104 | 1.3918 | 0.941 | 0.90761 | 0.81299 | 0.31206
Standard Curve
BCA Assay
Notes: peptide bonds reduce cupric ions to cuprous ions,
Bicinchoninic acid binds to cuprous ions
conc started at 15mg/ml

## Slide 16
Degradation Totals
  Polymer A and Protein B degrade simultaneously
  Decrease in rate of degradation over time
  Covalently linked components
15
Chart: Time (h)
| 1 | 2 | 4 | 7 | 24 | 48 | 72 | 96 | 120 | 144
Polymer A | 5.4646 | 11.851 | 20.8933 | 34.4007 | 48.393 | 67.0206 | 81.7241 | 88.7465 | 95.3487 | 99.3353
Protein B | 7.3355 | 16.1128 | 25.2986 | 41.2065 | 49.2942 | 65.2204 | 75.6984 | 84.9301 | 93.8873 | 98.5846
Cumulative Percent Release during Degradation
Notes: a - started at 45mg/ml
b - conc started at 15mg/ml

## Slide 17
  Varying temperature for hydrogel storage resulted in faster degradation time: 5 days with a heat cool cycle compared to 7 days without
  SDS-PAGE confirmed the presence of components A and B in supernatant as expected
  Polymer A and Protein B had similar degradation patterns and reached 50% release at 24 hours, compared to 30% for control groups
Conclusions
16

## Slide 18
  Confirm composition of degradation
    Test for micelles in the supernatants throughout the study using Dynamic Light Scattering (DLS)
  See if thermocycling affects degradation and efficacy of drug-loaded hydrogel
Future Considerations
17

## Slide 19
  Thomas Lab
  Marianne Esnaurrizar
  Dr. Emily Roe
  Dr. Megan Elliott
  Maya Levitan
  Nathan Holland
  SUIN Program Directors
  Dr. Mikkel Thomas
  Leslie O’Neill
Acknowledgements
18
This research was funded by NSF Award #2349519 and ARPA-H agreement #AY2AX000135