## Slide 1: Optimization of Poly(Ethylene Glycol)-Vinyl Sulfone (PEG-VS) Hydrogels for Enhanced Extracellular Vesicle Biomarker Detection
By: Amaris Mbuagbaw
PI: Dr Jina Ko
Mentor: Emily Huynh

## Slide 2: Extracellular Vesicles
20–200 nm membrane-bound vesicles released by most cell types into biofluids (blood, urine, saliva), enabling minimally invasive sampling.
Carry proteins, lipids, DNA, mRNA, and miRNA that reflect the physiological or pathological state of the parental cell, making them valuable disease biomarkers.
Cross biological barriers, including the blood–brain barrier, providing insight into neurological diseases and even cancer
Low abundance and nanoscale size make traditional amplification techniques more challenging
Parent Cell
Recipient Cell
Extracellular Vesicle
Cargo:
-Nucleic acids
-proteins
- lipids

## Slide 3: EV Detection and Optimization
Rolling Circle Amplification (RCA): Isothermal DNA amplification technique for detection of low-abundance targets without PCR thermal cycling or amplification bias.
PEG-VS hydrogels: Semipermeable matrix enabling target diffusion and stable probe immobilization to model EV biomarker detection.
Pre-RCA optimization: Systematic optimization of hybridization and ligation conditions to maximize downstream RCA detection.
Improved EV Detection
Optimized pre-RCA conditions

## Slide 4: Hydrogel Fabrication and Functionalization
PEG-VS precursor, TEA, HFE-7500 and TCEP-reduced Cy3-thiolated miR-21 were loaded into a flow-focusing microfluidic device (~200 Hz) to generate 60µm droplets.
TCEP reduction exposed free thiol groups, enabling covalent bonding of the miR-21 probes to the vinyl sulfone (VS) groups of the PEG hydrogel.
TEA promotes crosslinking of the PEG-VS precursor.
Crosslinked functionalized PEG-VS hydrogels are demulsified and washed.
8 hours crosslinking
Functionalized hydrogel
Hydrogel matrix
Probe

## Slide 5: Hydrogel Fabrication and Functionalization
Flow rates: Aqueous phase 0.1 µL/hr and dispersed phase 0.5 µL/hr (1:5 ratio)
Average hydrogel diameter: 51.5 µm
Coefficient of variation (CV): 2.46%
Low CV confirms highly uniform and reproducible hydrogel fabrication
Fig 1:Droplet Formation
Fig 2:Precursor gels
Fig 3:Crosslinked functionalized gel
60µm

## Slide 6: Testing Capture efficiency
Hybridization: 1× TET + NaCl buffer with miR-21 target
Target concentrations: 1 µM → 1 pM
Mean Fluorescence intensity decreased with target concentration
<10 nM: minimal detectable fluorescence
1µM
1µM
100nM
10nM
1nM
1pM
neg
60µm
60µm
60µm
60µm
60µm
60µm

## Slide 7: Testing Ligation Conditions
Ligation is the key pre-RCA step, generating the circular DNA template required for phi29-mediated signal amplification.
Temperature and incubation time were optimized to maximize padlock probe circularization.
Mean fluorescence intensity (MFI) was used to evaluate ligation performance

## Slide 8: Temperature Optimization
37C
RT
Neg
Room Temperature (RT) and 37°C ligation conditions were compared alongside a negative control.
RT yielded the highest mean fluorescence intensity (MFI).
Results demonstrate that ligation efficiency is influenced by reaction temperature.
60µm
60µm
60µm

## Slide 9: Ligation Time optimization
30 mins, 1 hour, and 2hour ligation times were evaluated alongside a negative control.
The highest mean fluorescence intensity (MFI) was observed after 30 minutes of ligation.
Increasing ligation time did not enhance fluorescence, indicating that 30 minutes was sufficient for effective ligation.
30 mins
1hr
2hr
Neg

## Slide 10: Conclusion and Future directions
Summary
PEG-VS hydrogels: Reproducible platform for systematic RCA optimization.
Target detection limit: Measurable fluorescence at ≥10 nM.
Optimal ligation temperature: Room temperature (~25 °C) (highest MFI).
Optimal ligation time: 30 min; extended incubation provided no additional benefit.
Future Directions:
Optimize additional pre-RCA parameters: T4 DNA ligase concentration, buffer composition (pH,)
Validate the optimized workflow using extracellular vesicle (EV) samples.

## Slide 11: Acknowledgements
Mentorship:
Emily Huynh, Jenlu Pagnotta, Dr Ashley Wallace,
Dr Adriana Santiago-Ruiz
PI:
Dr Jina Ko
This work was carried out in part at the Singh Center for Nanotechnology, which is supported by the NSF National Nanotechnology Coordinated Infrastructure Program under grant NNCI-2025608, and through the use of facilities supported by the University of Pennsylvania Materials Research Science and Engineering Center (MRSEC) DMR-2309043.