## Slide 1: Magneto-optic imaging of Ferromagnetic Thin Films
Leo Turner, University of Alabama
Dr. Shireen Adenwalla, University of Nebraska - Lincoln Rabindra Oliya, University of Nebraska - Lincoln
NSF Award ID #1950137

## Slide 2: Magnetic Domains
https://commons.wikimedia.org/wiki/File:NdFeB-Domains.jpg

## Slide 3: Magneto-Optic Kerr Effect (MOKE)
Measures magnetic hysteresis loops of thin films
Polarized light reflects off a magnetized material, and the polarization changes based on the magnetization of the material, allowing for easy measurement

## Slide 4: MOKE Setup
Can measure magnetic susceptibility and other constants using a simple laser setup
Magnetic field can be applied to the sample in-plane (LMOKE) or out of plane (PMOKE). Comparison between the two can find the easy axis of the thin film.
Polarizer
Sample
Analyzer
Detector
PMOKE LMOKE

## Slide 5: MOKE Microscope
Can measure magnetic domain walls using a camera and some signal processing
Before signal processing – scratches and optical aberrations are visible

## Slide 6: Skyrmions
Skyrmions are a swirling magnetic
texture.
These textures are a focus of study because of their stability and their potential to manipulated by current and other means.
Balance of the Dzyaloshinskii – Moriya interaction (perpendicular) and exchange interaction (parallel).
Schütte & Garst (2014)
MOKE Skyrmion images in similar film, with decreasing magnetic field applied.
Jiang et al, Blowing magnetic skyrmion bubbles

## Slide 7: Samples
Our samples used CoFeB as the Ferromagnetic layer of our thin film, with varying thicknesses to vary the magnetic constants of the film.
 | Pt (2 nm) | 
 | CoFeB (0.4-0.6 nm) | 
 | Pt (2 nm) | 
 | Ta (1 nm) | 
 | Cr (2 nm) | 
Silicon/Lithium Niobate Substrate |  | 
- Ta dusting – under 1 Angstrom

## Slide 8: Image Processing
MatLab is used to do image processing.
We need to balance intensity across the image, remove optical aberrations, and distinguish between up and down domains
Large amounts of data
The microscope automatically takes a base image and subtracts it from the rest of the images.

## Slide 9: Adaptive Histogram Equalization and 2-D Median filter

## Slide 10: Background subtraction

## Slide 11: Image binarization
Thresholding values

## Slide 12: Morphological Opening and Closing Operations
Udacity on YouTube

## Slide 13: Final Images
Stripe domains
Bubble domains
“Dendritic” domains