## Slide 1
Photodegradable Sacrificial Templates for Embedded Microchannels
Nicolas E. Manning
PI: Paul A. Kohl
Mentor: Jose Lopez Ninantay
SUIN REU 2026
Notes: Add more words in a few spots.

## Slide 2
What are Embedded Microchannels?
Small pathways that move liquids or gases through a device.
Sensors, microfluidics, and electronics
Embedded microfluidic channels.
Image: L. Tran, “Microfluidics: Biology’s Liquid Revolution,” The Scientist.

## Slide 3
The Sacrificial Template Strategy
3

## Slide 4
Light-Triggered PPC Depolymerization
PAG = photoacid generator:
4
acid + byproducts
Film-casting
Photo-exposure
Dry-development
Incident photons
Poly(propylene carbonate)
Products
248 nm

## Slide 5
Research Question
Can photoacid generation be extended to 375 nm (near-UV)?
5
Rhodorsil-FABA (PAG)
CPTX (sensitizer)
Prevailing chemical species:
Approach 1: 365 nm (i-line) PAGs
Approach 2: Chemical Sensitization
Approach 2: Chemical Sensitization

## Slide 6
Experimental Overview
6
Prepare PPC formulations
Coat films on wafers
Expose and heat
Measure removal and pattern quality
1
2
3
4

## Slide 7
Finding a Working Formulation
Tested many different formulations
Grouped by outcome
Working mixtures selected for characterization
7
Chart: 
Partial removal
Complete removal
Height Profile Traces:

## Slide 8
Chart: Dose (mJ/cm2)
| 10 | 35 | 60 | 85 | 110 | 135 | 300 | 550 | 800 | 1050 | 1300 | 1550 | 1800 | 2050
 | 1 | 1 | 1 | 0.95987 | 0.92216 | 0.85297 | 0.14853 | 0.015218 | 0.0118 | 0.0061828 | 0.00056557 | 0.0033515 | 0.0051215 | 0
Quantifying Effective Exposure
Use contrast curves
Quantifies how efficiently a film clears as exposure dose increases
8
=
D0 = Dose that clearing begins
D100 = Dose that fully cleared
D0
D100
Clearing
starts
Fully cleared
Notes: Spend more time here and say how this is also how photoresists are quantified.

## Slide 9
Chart: Dose (mJ/cm2)
| 50 | 400 | 750 | 1100 | 1450 | 1800 | 2150 | 2500 | 2850
0.25 wt% sensitizer | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
0.5 wt% sensitizer | 1 | 1 | 1 | 1 | 1 | 0.98661 | 0.96935 | 0.95909 | 0.95556
1 wt% sensitizer | 1 | 1 | 1 | 1 | 1 | 0.98948 | 0.9789 | 0.96583 | 0.95369 | 0.95003 | 0.92166 | 0.91416 | 0.70064 | 0.55661 | 0.49251 | 0.46884 | 0.34954 | 0.21915 | 0.1423 | 0.076657 | 0 | 0.013582 | 0.020914
1.5 wt% sensitizer | 1 | 0.86219 | 0.65397 | 0.60656 | 0.41889 | 0.4026 | 0.25946 | 0.11231 | 0.092277 | 0.05884 | 0.025541 | 0.02115 | 0.018594 | 0.017485 | 0.010562 | 0.014546 | 0.0073563 | 0
4.5 wt% sensitizer | 0.99792 | 0.9 | 0.83181 | 0.59985 | 0.56457 | 0.44906 | 0.37908 | 0.36957 | 0.30243 | 0.16962 | 0.065517 | 0.054733 | 0.0458 | 0.034373 | 0.020267 | 0.019917 | 0.017373 | 0.01378
248 nm PAG-only control | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 0.99392 | 0.96668 | 0.95479 | 0.90505 | 0.90627 | 0.82356 | 0.79218 | 0.688 | 0.69083 | 0.55742 | 0.40007 | 0.34025 | 0.08884 | 0.02281 | 0.01772
Tuning the Process
9
Control (248 nm)
Increasing sensitization with constant PAG concentration reduces required dosage
Lowest concentration
Highest concentration
Notes: with 248 nm sample, compare this with longer y
Find a way to describe what is different between each colored line.

## Slide 10
Chemical Scheme
10
CPTX-sensitized photoinduced electron-transfer pathway.

## Slide 11
Testing Pattern Quality
Higher doses increase clearing rate
Longer development widens features
Thicker films amplify widening
11
Film thickness (µm) | Development time (min) | Widening (µm)
10 | 10 | 45
10 | 30 | 110
36 | 10 | 100
36 | 30 | 130
Notes: Data is for 10 um, include 36 um data.

## Slide 12
Summary
Shifted the process from deep-UV to more accessible near-UV radiation
Sensitization approach was successful
Additives found optimal at 1:1 molar ratio
Dose, development, and thickness trade-offs
Deep-UV
(248 nm)
Near-UV
(375 nm)
12
Rhodorsil-FABA (PAG)
CPTX (sensitizer)
Higher dose = faster film clearing, more acid
Greater development time = feature widening
Thicker films = amplified lateral widening

## Slide 13
Manuscript Submitted
Photopatterning Poly(propylene carbonate) Sacrificial Films with Photoacid Generator and 375 nm Sensitizer
Nicolas E. Manning, Jose Lopez Ninantay, Paul A. Kohl
Submitted to: Journal of Micro/Nanopatterning, Materials, and Metrology
Status: In-review
13

## Slide 14
Acknowledgements
PI: Professor Paul A. Kohl
  Opportunity to conduct this research.
Mentor: Jose Lopez Ninantay
  Training and guidance
Georgia Tech SENIC/SUIN REU Program
  Leslie O’Neill, Dr. Mikkel Thomas
National Science Foundation, and Program/Project Sponsors
  Supporting the REU program and this research.
Paul A. Kohl
Jose Lopez Ninantay
14

## Slide 15
Connect with me!
Thank you!