## Slide 1
Raman Spectroscopy to Characterize Diamond
Quantum Sensors
Jessen Carriveau
Mentor: Professor Robert Nemanich
Photo by Franz Koeck

## Slide 2
Jessen A. Carriveau
Phoenix, Arizona
ASU Physics Undergraduate
Honors Thesis and REU project with Prof. Robert Nemanich
About Me

## Slide 3: Nitrogen Vacancy Center (NVC)
What are they?
Carbon lattice defect with nitrogen substitution and adjacent vacancy
Physical Characteristics:
Spin-1 color center
Measured with visible light (ODMR)
Magnetic resonance spectrum at room temperature
1 T. Wogan, and P. Allen, “Putting a New Spin on Things,” Chemistry World, (2017).
3D View
2D View

## Slide 4: NV0 vs NV-
NV0 – “neutral” charge state, N atom has 5 valence electrons
NV- – “negative” charge state, extra electron in vacancy forms spin-1 pair with a valence electron. Ideal for our applications.
7 A. Haque, and S. Sumaiya, “An Overview on the Formation and Processing of Nitrogen-Vacancy Photonic Centers in Diamond by Ion Implantation,” Journal of Manufacturing and Materials Processing (JMMP) 1(1), 6 (2017).

## Slide 5: NVC Applications
Quantum Computing “Qubits”
Quantum alternative to the classical “bit"
Quantum Sensors
Robust temperature, electric field, and magnetic field sensors at nanoscale
2 Quantum Brilliance, “Applications,” Quantum Brilliance, (2026)

## Slide 6: Why Diamond?
High Thermal Conductivity
~10x better than silicon 4
Ultrawide-Bandgap
Conduction/Valence bands do not interfere with NVC electronic state 5
Electrical Properties
High electron mobility (4500 cm2/V*s) and breakdown field (10 MV/cm) 6

## Slide 7: The Problem
How do we maximize the number of NVCs in our diamond?
NVC density variables:
Diamond growth method
Location on diamond
Depth in diamond
Plasma-Enhanced Chemical Vapor Deposition (PECVD) machine
Diamond wafer growing in PECVD machine
Photos by Franz Koeck

## Slide 8: Raman Spectroscopy
Identifies chemical structure by detecting changes in photon energy due to molecular vibrations
Micro-Raman Grating Spectrometer
Microscope + Raman spectrometer
Variable gratings
Multiple laser wavelength settings
Nondestructive towards sample
Can gather photoluminescence (PL) spectra as well
3 Eyring Materials Center, “Raman Spectrometer (Custom Built Multi-Wavelengths),” Asu.edu, (2025).

## Slide 9: High Resolution Raman Spectrum

## Slide 10: Nitrogen-Doped High-Pressure, High Temperature (HPHT) vs Phosphorus-Doped PECVD

## Slide 11: “Spots” on Sample
1
3
2
4 mm
4 mm

## Slide 12: NVC Density at Varying Spots

## Slide 13: NVC Density at Varying Depths

## Slide 14: Conclusions
Growth Method
Phosphorus-doped PECVD gives stronger NV- peaks than nitrogen-doped HPHT
Location on Sample
NVC density appears to vary at different spots on sample, but the distribution depends on the sample
Depth in Sample
PL spectra show increasing NVC density with depth when Raman does not, so the data is inconclusive

## Slide 15: Future Work
We want to investigate the ratio of NV0 and NV- using just the micro-Raman grating spectrometer.
We are waiting on a blue (~450 nm) laser to do this.
8 G., D.J. McCloskey, A. Mameli, A.J. Healey, C. PattinsoThalassinosn, D. Simpson, B.C. Gibson, A. Stacey, N. Dontschuk, and P. Reineck, “Robust Quantification of the Diamond Nitrogen-vacancy Center Charge State via Photoluminescence Spectroscopy,” APL Photonics 10(10), (2025).

## Slide 16: Works Cited
1 T. Wogan, and P. Allen, “Putting a New Spin on Things,” Chemistry World, (2017).
2 Quantum Brilliance, “Quantum Brilliance,” Quantum Brilliance, (2026).
3 Eyring Materials Center, “Raman Spectrometer (Custom Built Multi-Wavelengths),” Asu.Edu, (2025).
4 F. Zhao, Y. He, B. Huang, T. Zhang, and H. Zhu, “A Review of Diamond Materials and Applications in Power Semiconductor Devices,” Materials 17(14), 3437–3437 (2024).
5 S. Arya, “Quantum Sensing 101: The Nitrogen-Vacancy Center in Diamond,” Medium, (2025).
6 M.H. Wong, O. Bierwagen, R.J. Kaplar, and H. Umezawa, “Ultrawide-bandgap semiconductors: An overview,” Journal of Materials Research 36(23), 4601–4615 (2021).
7 A. Haque, and S. Sumaiya, “An Overview on the Formation and Processing of Nitrogen-Vacancy Photonic Centers in Diamond by Ion Implantation,” Journal of Manufacturing and Materials Processing (JMMP) 1(1), 6 (2017).
8 G. Thalassinos, D.J. McCloskey, A. Mameli, A.J. Healey, C. Pattinson, D. Simpson, B.C. Gibson, A. Stacey, N. Dontschuk, and P. Reineck, “Robust Quantification of the Diamond Nitrogen-vacancy Center Charge State via Photoluminescence Spectroscopy,” APL Photonics 10(10), (2025).

## Slide 17: Acknowledgements & Contact Information
Thanks to:
Prof. Robert Nemanich
Prof. Antia Botana
Jessica Hauer
Dr. Douglas Daniel
Contact me via email:
jessencarriveau@gmail.com