## Slide 1: Design and simulation of opto-electronic flash memory
Andrew Fang1 | Advisor: Dr. Stanley Cheung2
1School of Electrical and Computer Engineering, Georgia Institute of Technology 2Associate Professor, Department of Electrical and Computer Engineering, North Carolina State University

## Slide 2: Grand Challenges: AI Workloads Strain Conventional Computing Architectures
Mehonic et al., “Brain-inspired computing needs a master plan”
Gholami, Amir et al. “AI and Memory Wall.” IEEE Micro 44 (2024): 33-39.
Stark et al., “Opportunities for integrated photonic neural networks”
Exponentially Increasing Compute Demand
Memory Wall and Interconnect Bandwidth
Energy Efficiency and Sustainability

## Slide 3: Optical AI/ML Accelerators Offer a New Paradigm to Match Workload Demands
Shastri, B. J., Tait, A. N., Ferreira de Lima, T., Pernice, W. H., Bhaskaran, H., Wright, C. D., & Prucnal, P. R. (2021). Photonics for artificial intelligence and neuromorphic computing. Nature Photonics, 15(2), 102-114.
Key Advantages
Data transmission at light-speed
Minimal RC delay or loss
Massively parallel data transmission
Near-instantaneous, one-shot calculation

## Slide 4
High Throughput Parallel Data Transmission
Wavelength-Division Multiplexing
Mach-Zehnder Interferometer
Photonic Flash Memory Cell
Matrix-Vector Multiplication
Compute-in-Memory Matrix-Vector Multiplication
Single Operation

## Slide 5: The Bottleneck: Memory Accesses and Electrical/Optical Conversions
https://medium.com/lightmatter/techniques-for-performing-design-verification-of-a-mixed-signal-digital-analog-and-optical-d0068c9ff868
Lightmatter Optical Compute Core
Model training requires constant memory accesses to retrieve weights and training data and to store outputs
Lack of a non-volatile memory technology with optical readout requires optical-to-electrical (O/E) and electrical-to-optical (E/O) conversions
These conversions fundamentally limit speed, bandwidth, and energy efficiency

## Slide 6: Opto-electronic Flash Memory: A Near-Term Solution
Key Advantages
Fully CMOS-Compatible
High-density
Well-established for storing weights and training datasets
Opto-electronic Flash Memory Cell
Cheung et al., Laser & Photonics Review (2024)

## Slide 7: Objectives
TCAD modeling: Developing Technology Computer-Aided Design (TCAD) models for rapid simulation of opto-electronic flash memory designs
Memory performance evaluation: Simulating programming, retention, and erase operations to characterize speed, retention, and optical performance
Dielectric stack engineering: Proposing a novel cell design incorporating bandgap-engineered tunnel-oxides[1] optimized for improved performance
[1] Hang-Ting Lue et al., "BE-SONOS: A bandgap engineered SONOS with excellent performance and reliability," IEEE International Electron Devices Meeting, 2005. IEDM Technical Digest, Washington, DC, USA, 2005, pp. 547-550, doi: 10.1109/IEDM.2005.1609404.

## Slide 8: Opto-Electronic Flash Memory and the Plasma Dispersion Effect
Initial/Erased State (No Trapped Charge)
Programmed State (Charge Trapped & Channel Depleted)
Laser beam (unprogrammed)
Laser beam (programmed)
Optical Readout (Opto-electronic)
Charge Trapping (Flash)
Plasma Dispersion Effect
Quantum Tunneling
Electrostatic Repulsion

## Slide 9: Methodology & Simulation Setup
Technology Computer-Aided-Design (TCAD)
  Software: Silvaco ATLAS TCAD
  Simulates testing and device physics, providing internal insight to expose design flaws prior to fabrication
Simulated Internal Electric Field during Programming
Original Opto-electronic Flash Cell Design[1]
III-V/Si platform for integration of photonic devices on GaAs
Two HfO2 charge trap layers for trapping of electrons and holes, respectively
[1] Cheung et al., Laser & Photonics Review (2024)

## Slide 10: Simulation results
Initial
Programming
Retain
Erase
Return
+9V
-5V
Read
Read
Read

## Slide 11: Programming | +9V
Trapped Carrier Density During Programming Operation
Asymmetric Programming:
  Electrons: Early saturation in 10μs of trapped electrons with low trap occupancy (~1%)
  Holes: Later saturation of trapped holes with relatively higher trap occupancy (26.7% at t=1s)
Electron trap density: 1019 cm-3
Hole trap density: 8x1018 cm-3

## Slide 12: Retention | 0V | Read State
Hole Detrapping During Retention
Electron Detrapping During Retention
Effective Index Change During Retention
Poor carrier retention: Complete loss of trapped electrons within 10s and gradual 343x decrease in trapped hole density over one day timespan
Read-state volatility: Redshift followed by volatile blueshift consistent with hole de-trapping before settling to non-volatile state
Hole Detrapping
Electron Detrapping
Redshift following programming
Volatile blueshift
Non-volatile state
~1.16 days
~1.16 days

## Slide 13: Erase | -5V & Return | 0V
Trapped Hole Density Following Erase
Trapped Hole Density During Erase Operation
Initial equilibrium density
Initial equilibrium density
Complete erase: Initial and final state following 100ms erase show identical effective indices

## Slide 14: Device design
Original Device Design
Proposed Device Design

## Slide 15: Identified Performance Issues
Asymmetric programming
Poor carrier retention
Volatile read state
Original Device Design
Contributing Factor: III-V/Si Platform Integration
GaAs/Si Workfunction difference causes depletion of Si carriers with no applied voltage
Fundamentally limits programming efficiency
Carrier concentration changes contribute to read state volatility

## Slide 16: Bandgap-Engineered Tunnel Oxides Improve Speed and Retention Simultaneously
Initial/Retention State:
Programming (+9V):
Free carriers in channel and trapped carriers both face thick 5.6nm, energetically unfavorable barrier: Low tunneling rate
Programming voltage lowers band energy of second and third barrier
Tunneling electron experiences thin 1.6 nm barrier: High tunneling rate
Tri-layer Tunnel Oxide Structure

## Slide 17: Opto-electronic Cell Implementation
Tunneling Regimes in SiO2[1]
Proposed Design at +15V Programming (E = 13.2 MV/cm)
Proposed Design
[1] Hang-Ting Lue et al., "BE-SONOS: A bandgap engineered SONOS with excellent performance and reliability," IEDM (2005)
Layered P+/P- doping structure ensures high Si carrier density with minimal addition optical loss (25.72 mdB/cm)
Proposed Design at Retention

## Slide 18: CONCLUSION
Using TCAD modeling and simulation, performance deficiencies relating to the dielectric stack structure were identified in an initial opto-electronic Flash memory cell design.
A novel cell design using bandgap-engineered tunnel oxides is proposed to remedy these deficiencies, to be simulated in future work.
Acknowledgements
This work was partially supported by the Microelectronics Commons Program, a DoW initiative, under award number N00164-23-9-G059.
Distribution Statement A: Approved for public release. Distribution is unlimited.