## Slide 1: Aluminum Electrothermal MEMS Actuators
Presenter: Ryan Otten-Reimer
Mentor: Dr. Andrew Lingley
1
Notes: If you don't already know me, I'm Ryan and I'm working with Dr. Andrew Lingley this summer on fabricating thermal actuators

## Slide 2: Introduction
Microelectromechanical systems (MEMS)
  Tiny mechanical devices
  Utilize semiconductor fabrication processes
Electrothermal Actuator
  Thermal expansion via a current to expand beams
Applications
  Micromanipulation (biomedical)
  Micromirror stabilization
  RF switches
Transactions on Electrical and Electronic Materials (2024) 25:685–694
Notes: Motivation is to provide additional data to the field on aluminum MEMS devices, but mainly to provide more access to trainees

## Slide 3: Background
Why aluminum actuators?
  Ease of design and fabrication
  Lower cost
  Fast turnaround/prototyping
What's the best outcome?
  Encourage accessibility to semiconductor fabrication education
  Understand the applications and limits of aluminum-based MEMS devices

## Slide 5
Cross-section representation
Silicon wafer (500μm x 4mm)
*Colors may not be accurate, sizes are not to scale

## Slide 6
Deposit aluminum layer via electron beam evaporation.
Aluminum (~1μm)
Cross-section representation
*Colors may not be accurate, sizes are not to scale
Notes: Sublimation by using electron beam

## Slide 7
Photoresist (~1um)
Bake on a thin layer of photoresist, a non-soluble polymer that protects the wafer.
Cross-section representation
*Colors may not be accurate, sizes are not to scale
Notes: Protector for aluminum

## Slide 8
Ultraviolet
Photomask
The photomask is placed over the wafer and is exposed to UV light. The exposed photoresist goes through a chemical reaction that makes it soluble in developer.
Cross-section representation
*Colors may not be accurate, sizes are not to scale

## Slide 9
Cross-section representation
Wash away the soluble photoresist, revealing selected regions of aluminum.
Cross-section representation
Cross-section representation
Developer:
~2.5% Tetramethylammonium hydroxide (TMAH)
*Colors may not be accurate, sizes are not to scale
Notes: Developer (Tetramethylammonium hydroxide)

## Slide 10
Etch the unprotected photoresist to expose the silicon.
Cross-section representation
Aluminum etchant:
<80% Phosphoric Acid
<5% Acetic Acid
<5% Nitric Acid
*Colors may not be accurate, sizes are not to scale
Notes: Acid, phosphoric acid?

## Slide 11
Al
Silicon is etched by a plasma.
Plasma
Al
Cross-section representation
The shuttle is suspended by beams
*Colors may not be accurate, sizes are not to scale
Notes: Plasma is ionized gases like free fluorine radicals. Isotropic does not redeposit any protective gas layer and radicals bounce around

## Slide 12
Etched Silicon
Aluminum
AIP Conf. Proc. 1646, 25 (2015); doi: 10.1063/1.4908578
Top view
Shuttle
Anchors
Beams
*Colors may not be accurate, sizes are not to scale

## Slide 13
DC source is disconnected
Top view
Actuator beams experience thermal expansion due to resistive heating.
*Colors may not be accurate, sizes are not to scale

## Slide 14
DC source is connected
Actuator beams experience thermal expansion due to resistive heating.
Top view
*Colors may not be accurate, sizes are not to scale

## Slide 15: Characterization
Stylus Profilometer
Electron Microscope
Probing Station
Chart: Actuator Resistance
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1 | 1.2
 | 0 | 6 | 12 | 18 | 24 | 30 | 35 | 41 | 46 | 51 | 56 | 60 | 64 | 68 | 72 | 75 | 78 | 80 | 83 | 85 | 86 | 88
*surface profiling too
Notes: Critical stress is applied force over the cross sectional area (Max allowable force in pascals)

## Slide 18
Notes: Critical stress is applied force over the cross sectional area (Max allowable force in pascals)

## Slide 20: Modeling

## Slide 21: Modeling

## Slide 22: Modeling
Chart: Current (mA)
| 0 | 10 | 30 | 50 | 75 | 150
Analytical | 0 | 0.0625 | 0.56667 | 1.53 | 3.3767 | 12.2
Computational | 0 | 0.06 | 1.5 | 3.3 | 13.2
Chart: Beam Width (μm)
| 1 | 2 | 4 | 7 | 10 | 20
Analytical | 20 | 5.8 | 1.5 | 0.5 | 0.25 | 0.0625
Computational | 22.6 | 5.8 | 1.5 | 0.48 | 0.23 | 0.0528

## Slide 23: Conclusion
Aluminum MEMS actuators are fast to produce and require minimal training
A simple analytical model can predict displacement accurately
Films can be temperamental
Aluminum actuators actuate even under bad circumstances

## Slide 24: References
Baracu, A., Voicu, R., Müller, R., Avram, A., Pustan, M., Chiorean, R. S., Birleanu, C., & Dudescu, M. (2015). Design and fabrication of a MEMS chevron-type thermal actuator. AIP Conference Proceedings, 1646, 25-30. https://doi.org/10.1063/1.4908578
Heinke, R., Ehrhardt, M., Lorenz, P., & Klaus, Z. (2021). Dry etching of monocrystalline silicon using a laser-induced reactive micro plasma. Applied Surface Science Advances, 6, 100169. https://doi.org/10.1016/j.apsadv.2021.100169
Potekhina, A., & Wang, C. (2019). Review of Electrothermal Actuators and Applications. Actuators, 8(4), 69. https://doi.org/10.3390/act8040069
Pustan, M., Chiorean, R., Birleanu, C., Dudescu, C., Müller, R., Baracu, A., & Voicu, R. (2017). Reliability design of thermally actuated MEMS switches based on V-shape beams. Microsystems Technologies, 23, 3863–3871. https://doi.org/10.1007/s00542-015-2789-8
Ramya, S., Aravind, T., Kumar, S.P., & Ram, G. D. (2024). Design of Chevron Electrothermal Microgripper and its Prototyping Using SLM Based Additive Manufacturing. Transactions on Electrical and Electronic Materials, 25, 685–694. https://doi.org/10.1007/s42341-024-00552-1

## Slide 25
Thank you to Dr. Andrew Lingley and the Montana Microfabrication Facility.
This work was supported by National Science Foundation Grant 2349091 & 2025391.