## Slide 1
Characterization of Greener Cements by Scanning Electron Microscopy
Enmanuel Rijo
PI: Dr. Kimberly Kurtis
Mentor: Alan Wang

## Slide 2: Context

## Slide 3: Context
Portland cement is responsible for 5–8% of global human-made CO₂ emissions.

## Slide 4: Context
Portland cement is responsible for 5–8% of global human-made CO₂ emissions.
Calcination
Fuel combustion

## Slide 5: Context
+
Portland Cement
Blended limestone
ASTM C595 type IL Cement
=
Cement Ball Mill
1)
2)

## Slide 6: Context
Why Understanding Cement Microstructure Is Important?
Microstructure influences cement performance.
Grinding and mixing in enhancing performance.
Linking physical features to environmental and mechanical outcomes.
Enables comparative analysis of samples.

## Slide 7: Cement Minerals
Name | Mineral phase | Chemical Formula | Contribution
Tricalcium silicate | Alite () | 3CaO·SiO₂ | Dominates the first week strength (1–7 days).
Dicalcium silicate | Belite () | 2CaO·SiO₂ | Gives most of the later-age strength (>28 days).
Tricalcium aluminate | Celite () | 3CaO·Al₂O₃ | Contributes little direct strength.
Tetracalciumalumino ferrite | Ferrite () | 4CaO·Al₂O₃·Fe₂O₃ | Minor strength contributor.
Calcium sulfate dihydrate | Gypsum, hemihydrate, anhydrite | CaSO₄·2H₂O | It slows down the hydration process of cement.
Calcium carbonate | Calcite | CaCO₃ | GWP reduction
Name | Mineral phase | Chemical Formula | Contribution
Tricalcium silicate |  | 3CaO·SiO₂ | Dominates the first week strength (1–7 days).
Dicalcium silicate |  | 2CaO·SiO₂ | Gives most of the later-age strength (>28 days).
Tricalcium aluminate |  | 3CaO·Al₂O₃ | Contributes little direct strength.
Tetracalciumalumino ferrite |  | 4CaO·Al₂O₃·Fe₂O₃ | Minor strength contributor.
Calcium sulfate dihydrate | Gypsum, hemihydrate, anhydrite | CaSO₄·2H₂O | It slows down the hydration process of cement.
Calcium carbonate | Calcite | CaCO₃ | GWP reduction
Clinker
Added

## Slide 8: Context
Tools
Scanning Electron Microscopy (SEM)
High-resolution images
Reveals morphology
Energy Dispersive Spectroscopy (EDS)
Provides elemental composition
Support phase quantification and classification
Hitachi 8320 at Georgia Tech by Enmanuel Rijo

## Slide 9: Context
Sample Preparation
Cement on adhesive carbon tape
20nm layer of AuPd (60:40) for conductivity
SEM Settings
Voltage: 10 kV
Current: 30
Spot size: typically, around 50

## Slide 10: Context
Sample Preparation
Cement on adhesive carbon tape
20nm layer of AuPd (60:40) for conductivity
SEM Settings
Voltage: 10 kV
Current: 30
Spot size: typically, around 50

## Slide 12
SEM and EDS characterization
Study the morphology
Objectives
1
SEM Characterization to study the morphology
2
Identify and quantify elements with EDS
3
Gain a better understanding of chemical composition of type IL cements

## Slide 13: Work Done

## Slide 14
SEM

## Slide 15
SEM
Sample: HC04

## Slide 16
SEM

## Slide 17
EDS

## Slide 18
Counts
keV
EDS
The unlabeled picks correspond to the 20nm conductive layer of AuPd.

## Slide 19
Chart: %weight of elements
| CM01 | HC05 | AR02 | AR01 | TA01 | CM02 | AG02 | AG06 | HC04 | CM03 | AG01 | AG04 | BU01
Ca | 34 | 37.9 | 35.2 | 36.4 | 37.4 | 35.8 | 40.3 | 40.8 | 37.8 | 34.4 | 40.8 | 35.9 | 35.2
Si | 5.28 | 5.73 | 4.9 | 5.43 | 6 | 5.57 | 5.97 | 5.07 | 5.8 | 5 | 5.98 | 5.23 | 5.5
C | 14.4 | 11.9 | 11.8 | 13.3 | 11.9 | 12.5 | 10.2 | 12.1 | 11.4 | 12 | 9.93 | 9.17 | 12.2
S | 2.55 | 2.4 | 3.1 | 2.28 | 2.13 | 2.77 | 2.07 | 2.5 | 2.63 | 4.7 | 2.5 | 2.43 | 3.3
Fe | 1.95 | 2.3 | 1.53 | 1.95 | 1.83 | 1.93 | 2.1 | 1.53 | 1.83 | 2.9 | 2.05 | 1.87 | 2.5
K | 1.44 | 1.07 | 0.2 | 0.8 | 1.57 | 1.4 | 0.3 | 0.333 | 1.4 | 1.1 | 0.325 | 1.17 | 0.9
Al | 1.23 | 1.73 | 1.47 | 1.45 | 1.9 | 1.2 | 1.43 | 1.633 | 1.5 | 2 | 1.38 | 1.27 | 1.4
Mg | 0.325 | 0.933 | 0.3 | 1.13 | 0.7 | 0.333 | 1.3 | 0.2 | 0.767 | 0.3 | 1.25 | 0.6 | 1.4
Na | 0.1 | 0.1 | 0 | 0.1 | 0.1 | 0.1 | 0.0667 | 0.1 | 0.167 | 0.1 | 0.075 | 0.1 | 0.1

## Slide 20
Conclusions
Consistent major chemistry. Calcium (≈ 35–41 wt %) and silicon (≈ 5–6 wt %) dominate every sample, giving Ca/Si mass ratios of ≈ 6–7.
Limestone addition confirmed. Carbon contents of 9–14 wt % correspond to ~10–15 % calcite.
Minor elements stable. S, Fe, Al, K, Mg, and Na each remain below ~5 wt %, with limited scatter, indicating uniform raw‑mix control and grinding practice across plants.
Inter‑plant variability low. The spread in Ca and C is <5 wt %, suggesting that despite different production sites (CM, HC, AR, TA, AG, BU series), overall chemical composition is tightly clustered.

## Slide 21
Future Recommendations
Using a tape or adhesive made from a material not found in cement for EDS analysis.
Future Work
To translate compositional insights into performance metrics, the next phase will involve electrical resistivity testing of the same cement powders. These measurements will help to explore how the observed cement composition and limestone content influence ionic transport and durability.

## Slide 22
References
Briki, Y., Zajac, M., Ben Haha, M., & Scrivener, K. L. (2021). Impact of limestone fineness on cement hydration at early age. Cement and Concrete Research, 147, 106515.https://doi.org/10.1016/j.cemconres.2021.106515
Poudyal, L., Adhikari, K., & Won, M. (2021). Mechanical and durability properties of Portland‑limestone cement (PLC) incorporated with nano calcium carbonate (CaCO₃). Materials, 14(4), 905. https://doi.org/10.3390/ma14040905

## Slide 23: Acknowledgments: Ms. Leslie O’Neill Dr. Mikkel Thomas Dr. Kimberly Kurtis Alan Wang Collins Twum
Thank you!